| Colour | Product Code | Pack Size | Box Qty |
| --- | --- | --- | --- |
| Buff | GEOFIX20BF | 20Kg | 1 |
| Grey | GEOFIX20GY | 20Kg | 1 |

Product Description

GEO-FIX PAVING JOINTING COMPOUND is a unique ready to use self curing jointing material for all types of paving having joints of 5mm and over. GEO-FIX PAVING JOINTING COMPOUND is a quick and easy way of applying a permanent rigid joint with no special machinery or equipment required. GEO-FIX PAVING JOINTING COMPOUND is suitable for natural stone, concrete, slate, clay, terracotta and granite and can be used in areas subject to light vehicular traffic.

Benefits

- Supplied ready to use, no mixing required.

- Simply brush into joints and compact.

- Cement free.

- Sets hard, wont crack or wash out.

- Resists weeds and plant growth.

- Totally weatherproof, unaffected by frost.

- For all joints of 5mm wide and over.

- Water permeable, allows water to escape.

Areas For Use

- Footpaths.

- Outdoor patio areas.

- Indoor stone floor areas.

- Pedestrian areas.

- Driveways.

Limitations

- Do not use on joints smaller than 5mm.

- Read all instructions and leaflet carefully before use.

- Joint depth must be a minimum of 25mm

- Do not apply to wet areas or when rain is imminent or below 00C

- In areas subject to vehicular traffic it is essential that the paving elements are bedded on a class 1 mortar and a high percentage of the mortar is squeezed up the joint, thereby providing support for the paving elements.

- GEO-FIX should be considered for its aesthetic and not its structural properties.

- The jointing should not be cleaned by use of high pressure washers until cured for 7 days. The distance between nozzles to jointing must be at least 10cm.

- Due to natural variations in sand shade occasional colour difference may occur between batches. For large applications where multiple buckets may be used always use the same batch of material to ensure consistency of colour.

- Always follow the manufacturer’s instructions carefully. As the company cannot be aware of all the applications and materials the product may be used on, it is the user’s responsibility to determine suitability for use. Please contact technical services for advice or request technical data sheet.

Surface Preparation

Ensure that the paving to be jointed is dry and free from loose dirt, oil, debris and grease etc. it is essential the joint widths are a minimum of 5mm wide with a minimum depth of 25mm. deeper joints can be filled with dry sand or other materials to meet the required minimum depth.

Application

GEO-FIX is supplied ready to use and does not require any further mixing or addition of other materials.

Carefully open the vacuum packed bag and sprinkle GEO-FIX PAVING JOINTING COMPOUND sufficient to cover an area of 4-5m2 (see coverage table below). Using a soft brush, push the GEO-FIX PAVING JOINTING COMPOUND into the joints ensuring they are filled with the material.

Protect treated joints from rain until fully cured. Any contact with rain and water before the compound has set will affect the product.

To ensure a perfect joint, press the GEO-FIX PAVING JOINTING COMPOUND into the joints with a pointing tool or compact into joints using a vibrating plate. Top up as necessary.

Any residue left on the surface when cured can be simply cleaned off by sweeping with a stiff brush.

Coverage

(The figures given below are approximate quantities required at 25mm depth per 20kg of Geofix)

| Joint width | 250 x 250mm | 450 x 450mm | 600 x 600mm |
| --- | --- | --- | --- |
| 5mm | 13.0m2 | 22.0m2 | 26.5m2 |
| 6mm | 11.0m2 | 19.0m2 | 22.0m2 |
| 7mm | 9.0m2 | 16.5m2 | 17.5m2 |
| 8mm | 7.8m2 | 14.5m2 | 16.5m2 |
| 9mm | 6.5m2 | 12.0m2 | 14.5m2 |
| 10mm | 5.8m2 | 11.0m2 | 13.0m2 |

Specific Data

| Material | Ready to use sand mixture with Polybutadiene bonding agent |
| --- | --- |
| Density (approx) | 1.70 g/cm³ |
| Colour | Beige / grey |
| Packaging | 7.5kg and 20kg hermitically sealed vacuum packed foil bags |
| Joint Width | Minimum 5mm |
| Min Joint Depth With Foot Traffic | Minimum 25mm |
| Min Joint Depth With Light Vehicular Traffic | Minimum 40mm |
| Working Temperature | 0 to +40°C |
| Workability Duration | Approx 45 minutes @ 23°C. Higher temperatures reduce working time |

Compressive Strength (Nmm²)

|  | Sand Cement Mortar | Geo-Fix |
| --- | --- | --- |
| 1 Day | 4 | 6 |
| 7 Days | 8 | 12 |
| 28 Days | 13 | 18 |

Flexural Strength (Nmm2 )

|  | Sand Cement Mortar | Geo-Fix |
| --- | --- | --- |
| 1 Day | 5 | 6 |
| 7 Days | 11 | 14 |
| 28 Days | 13 | 15 |

Health & Safety

Consult MSDS for full list of hazards.

Storage

Store in a cool dry place. Protect packaging from punctures or piercings. Any exposure to air will start the curing process. Do not store in direct sunlight.

Shelf Life

24 months from date of manufacture when stored in unopened containers in accordance with manufacturer’s instructions.

The technical data contained herein is based on our present knowledge and experience and we cannot be held liable for any errors, inaccuracies, omissions or editorial failings that result from technological changes or research between the date of issue of this document and the date the product is acquired. Before using the product, the user should carry out any necessary tests in order to ensure that the product is suitable for the intended application. Moreover, all users should contact the seller or the manufacturer of the product for additional technical information concerning its use if they think that the information in their possession needs to be clarified in any way, whether for normal use or a specific application of our product. Our guarantee applies within the context of the statutory regulations and provisions in force, current professional standards and in accordance with the stipulations set out in our general sales conditions. The information detailed in the present technical data sheet is given by way of indication and is not exhaustive. The same applies to any information provided verbally by telephone to any prospective or existing customer.

# Text boxes

GEO-FIX PAVING JOINTING COMPOUND