| Colour | Product Code | Pack Size | Box Qty |
| --- | --- | --- | --- |
| Natural Stone | GEOWET14STONE | 14kg | 1 |
| Anthracite | GEOWET14ANTH | 14kg | 1 |
| Slate Grey | GEOWET14GY | 14kg | 1 |

Product Description

Geo-Fix( All Weather Jointing Compound is a unique, ready to use jointing material for all types of paving having joints of 6 mm and over that can be used in both dry and wet conditions. Geo-Fix( All Weather Jointing Compound is a quick and easy way of applying a rigid joint on most common paving types including Natural Stone, Concrete, Slate, Clay, Terracotta and Granite.

Benefits

- Supplied ready to use, no mixing required.

- Can be used in both wet and dry conditions.

- Simply brush into joints and compact.

- Cement free.

- Sets hard, wont crack or wash out.

- Resists weeds and plant growth.

- Totally weatherproof, unaffected by frost.

- For all joints of 6mm wide and over.

- Water permeable, allows water to escape.

Areas For Use

- Footpaths.

- Outdoor patio areas.

- Indoor stone floor areas.

- Pedestrian areas.

- Driveways subject to light occasional vehicular traffic.

Limitations

- Do not use on joints smaller than 6mm

- Do not apply to dry paving. The paving must be wetted prior to and during application.

- Read all instructions and leaflet carefully before use.

- Joint depth must be a minimum of 25mm

- Do not apply below 30C or if the ground/paving temperature is below 30C.

- In areas subject to vehicular traffic it is essential that the paving elements are bedded on a class 1 mortar and a high percentage of the mortar is squeezed up the joint, thereby providing support for the paving elements.

- GEO-FIX should be considered for its aesthetic and not its structural properties.

- The jointing should not be cleaned by use of high pressure washers until cured for 14 days. The distance between nozzles to jointing must be at least 15cm and a fan nozzle must be used.

- Due to natural variations in sand shade occasional colour difference may occur between batches. For large applications where multiple buckets may be used always use the same batch of material to ensure consistency of colour.

- Always follow the manufacturer’s instructions carefully. As the company cannot be aware of all the applications and materials the product may be used on, it is the user’s responsibility to determine suitability for use. Please contact technical services for advice or request technical data sheet.

Surface Preparation

Ensure that the paving to be jointed is dry and free from loose dirt, oil, debris and grease etc. it is essential the joint widths are a minimum of 6mm wide with a minimum depth of 25mm. deeper joints can be filled with dry sand or other materials to meet the required minimum depth.

Application

GEO-FIX is supplied ready to use and does not require any further mixing or addition of other materials.

Wet the paving surface. The paving must be kept wet during application but free from standing water.   Failure to wet the paving surface will result in temporary staining.

Ensure that the areas where you are not working remain wet at all times.  This is particularly important in warm or hot weather conditions.

Carefully open the vacuum-packed bag and sprinkle sufficient Geo-Fix( All Weather Jointing Compound over the wet paving to cover an area of 2-3 m2 (see coverage table below).

Using a soft brush, push the Geo-Fix( All Weather Jointing Compound into the joints ensuring that they are filled with the compound.

The material MUST be compacted into the joints.

Compact Geo-Fix( All Weather Jointing Compound into the joints with a pointing tool. Top up and compact ensuring a fully compacted and topped up joint. Carefully sweep off any excess with a soft brush ensuring that the material is swept at a 450 angle to the joints.  Finish the surface decoratively giving a smooth flat finish with a pointing tool before moving onto the next area to be jointed.

Geo-Fix( All Weather Jointing Compound can withstand almost any amount of rain without the quality of the product being compromised.  Heavy rain may cause the smoothed surface of the joint to be disturbed that may require re-finishing.

Any residue left on the surface when cured can be simply cleaned off by sweeping with a stiff brush.

Material or residue that has been left exposed for more than 30 minutes should NOT be used, as it will be adversely affected.

Use Geo-Fix( All Weather Jointing Compound within 45 minutes of opening. In temperatures exceeding 25oC the material must be used within 30 minutes of opening the bag.

WATCHPOINTS

It is essential that all surfaces are wetted prior to application, and joint widths are a minimum of 6mm wide and a minimum of 25mm deep. A trial area should always be undertaken prior to full scale application. Whilst Geo-Fix All Weather Jointing Compound eliminates the staining problems associated with using sand/cement mortars by not sticking to the paver it should be noted that on certain types of paving, differences in porosity, texture and colour may be highlighted by using the jointing compound. Geo-Fix All Weather Jointing Compound is not suitable for joints subjected to continuous water immersion and is not suitable to fill to the top of chamfered joints (N.B – always finish to level or below the start of the chamfer)

IT IS ESSENTIAL THAT GEO-FIX ALL WEATHER JOINTING COMPOUND IS FULLY COMPACTED INTO ALL JOINTS OTHERWISE POOR STRENGTHS WILL OCCUR.

Do not use this product on solids concrete beds without sufficient falls and water drainage.

Geo-Fix All Weather Jointing Compound should not be considered to have any structural properties; therefore it is important that there is no paving movement

Never leave the compound on the surface of paving for a period in excess of 30 mins as it will part cure, giving poor strength once compacted into joints and may give staining issues in area of contact.

Cement based pavers: This product may also highlight problems due to differential curing of cost effective cement based paving.

Coverage

(The figures given below are an approximate coverage based on a 14gk bucket)

| Stone Size | Joint Size 10mm(W) x 25mm(D) |
| --- | --- |
| 600mm x 600mm | 8.25 - 9m2 |
| 600mm x 450mm | 6.50 – 7.25m2 |
| 450mm x 450mm | 5.75 – 6.25m2 |
| 300mm x 450mm | 4.75 – 5.25m2 |
| 300mm x 300mm | 3.75 – 4.25m2 |

Specific Data

| Material | Ready to use sand mixture with Polybutadiene bonding agent |
| --- | --- |
| Drying time | 6-12 hours @ 20 Degrees C. |
| Colour | Natural Stone, Grey and Anthracite |
| Packaging | 14kg hermitically sealed vacuum packed foil bags |
| Joint Width | Minimum 6mm |
| Min Joint Depth With Foot Traffic | Minimum 25mm |
| Min Joint Depth With Light Vehicular Traffic | Minimum 40mm |
| Working Temperature | +3 to +40°C |
| Workability Duration | Approx. 45 minutes @ 23°C. Higher temperatures reduce working time |

Health & Safety

Consult MSDS for full list of hazards.

Storage

Store in a cool dry place. Protect packaging from punctures or piercings. Any exposure to air will start the curing process. Do not store in direct sunlight.

Shelf Life

24 months from date of manufacture when stored in unopened containers in accordance with manufacturer’s instructions.

The technical data contained herein is based on our present knowledge and experience and we cannot be held liable for any errors, inaccuracies, omissions or editorial failings that result from technological changes or research between the date of issue of this document and the date the product is acquired. Before using the product, the user should carry out any necessary tests in order to ensure that the product is suitable for the intended application. Moreover, all users should contact the seller or the manufacturer of the product for additional technical information concerning its use if they think that the information in their possession needs to be clarified in any way, whether for normal use or a specific application of our product. Our guarantee applies within the context of the statutory regulations and provisions in force, current professional standards and in accordance with the stipulations set out in our general sales conditions. The information detailed in the present technical data sheet is given by way of indication and is not exhaustive. The same applies to any information provided verbally by telephone to any prospective or existing customer.

# Text boxes

GEO-FIX ALL WEATHER PAVING JOINTING COMPOUND