| Colour | Product Code | Pack Size | Box Qty |
| --- | --- | --- | --- |
| Grey | STDFLEXIGY25 | 25KG | 1 |

Product Description

EVERBUILD STANDARD SET FLEXI is a cement based wall and floor tile adhesive with excellent adhesion and non-slip properties ideal for thin bed bonding of tiles to walls and floors. This flexible adhesive can be used internally and externally to fix a wide variety of tiles i.e. ceramic, porcelain, natural stone (except those susceptible to staining) and vitrified tiles to substrates such as concrete, cement, plaster, masonry, construction boards, screeds etc. Conforms to EN 12004 Class C2 TE.

Conforms to the requirements of EN 12004 for frost resistant and water-proofing. A flexible adhesive which includes longer open time properties for application in hard to reach areas.

Benefits

- For ceramic, porcelain, and stone (not sensitive to discolouration or deformation)

- Excellent adhesion to concrete, cement, plaster, construction board etc.

- Slip resistant

- Waterproof and Frost resistant

- Suitable for use with underfloor heating

Areas for Use

- Bonding wall and floor tiles.

- Internal/External use.

- Recommended for tiling domestic, communal areas.

- Tiling onto common building substrates including concrete, cement screeds, plaster, masonry, construction boards and old ceramic tiles.

Limitations

- Do not use on natural stones (e.g. travertine, marble etc.) which are sensitive to discolouration.

- Do not apply if ambient temperature is below 5oC.

- Do not walk on floors for 24 hours after application.

- Do not mix more material that can be handled in 3 hours.

- Do not attempt to re-constitute the mix with water once setting has occurred.

- It is the user’s responsibility to determine suitability for use. If in doubt contact Technical Services for advice.

Surface Preparation

Ensure adequate dryness, strength, bearing strength, evenness and dimensional stability. Ensure the substrate is free of residues which reduce adhesion, e.g. dust, dirt, oil, fat and loose particles. Surface treatments or any "friable" areas of the subfloor must be mechanically removed and the subfloor repaired with Everbuild levelling compounds as required.

Substrate should fulfil the requirements of DIN 18 202, tolerances in building constructions. With subsequent installation of ceramic coverings cement screeds are required to be at least 28 days old and to display a residual moisture reading of < 2.0 CM-% (heating screeds < 2.0 CM%), calcium sulphate screeds should have a reading of < 0.5 CM-% (heating screeds <0.3 CM-%).

If used on above mentioned substrates in moist or wet rooms, the application of the Everbuild Aquaseal Wet Room System has to be performed.

Priming

It is recommended that all porous, weak or dusty substrates be primed with Everbuild S.B.R.

Application

Using a clean receptacle, add EVERBUILD STANDARD SET FLEXI to cold clean water to form a homogeneous mixture (approximately 6.75ltrs of water per 25kg of Standard Set Flexi). Use of a mixer with 600 rpm is recommended. Do not mix more material than can be handled within 3 hours. The mortar is to be applied and brushed off using a suitable notched trowel. The material to be laid is inserted and pressed into the fresh bed of adhesive while it is still wet. Remove wet mortar residues with Everbuild Wonder Wipes.

Unevenness up to 5 mm can be levelled with EVERBUILD STANDARD SET FLEXI.  We recommend Everbuild floor levelling compounds for full-surface levelling.

Material that has already been set can-not be re-mixed with additional water or powder.

Immediately after use clean tools with water.

EVERBUILD STANDARD SET FLEXI is suitable for application by floating, buttering and/or floating-buttering method according to DIN 18 157.

For large-sized fully vitrified tiles > 30 x 30 cm on floor surfaces we recommend using Everbuild PTB Adhesive with a flowing consistency for nearly cavity-free bonding especially on heated constructions. If a mortar with flowing consistency is not used for laying large-sized fully vitrified tiles > 30 x 30 cm, we recommend applying a thin contact layer on the backside of the tiles with the corresponding thin-bed mortar. For large-sized fully vitrified tiles apply a thin contact layer on the backside of the tiles with EVERBUILD STANDARD SET FLEXI.

In case of laying highly absorbent Chinese granite (e.g. Padang) irreversible discolouration can appear. We recommend a test bonding. For exterior areas use only suitable natural stones.

Do not use on natural stones (ie travertine, marble etc) that are sensitive to discolouration.

The laying of ceramic tiles and slabs and natural stones on hollow floors without a screed as additional burden- sharing layer, should not be done without the approval of the planner for the hollow floor and the designated covering. It is to use a thin-bed mortar of the category C2 S1 with the buttering-floating method or an Everbuild floor adhesive of the category C2 S1 with flowing consistency. For sizes from 40 x 40 cm it is necessary to apply a contact layer on the backside of the tiles.

Protect EVERBUILD STANDARD SET FLEXI during the working process from high ambient temperatures, direct sunlight and draughts, as this will affect the open time. Watch for skin formation when working in adverse conditions.

When applying externally the work area should be protected from rain, frost and extremes of temperature until cured. Do not apply if ambient temperature is less than 5°C. The working and curing process is accelerated by high temperatures and decelerated in low temperatures.

Specific Data

| Appearance | fine grey powder |
| --- | --- |
| Open Time (EN1346) | 30 minutes |
| Application Temp | +5oC to 35oC |
| Service Temp | -20 to +80oC. |
| Pot Life | 3 hours @20oC |
| Bed Thickness | 5mm |
| Setting Time | Foot traffic after 24 hours |
| Storage | Store in cool dry conditions. |
| Coverage | with 6 mm notched trowel approx. 2.5 kg/m2 with 8 mm notched trowel approx. 3.0 kg/m2 with 10 mm notched trowel approx. 3.5 kg/m2 |

Health & Safety

Consult MSDS for full list of hazards.

Storage

Store at moderate temperatures. PROTECT FROM DAMP

Shelf Life

12 months from date of manufacture when stored according to manufacturer’s instructions.

The technical data contained herein is based on our present knowledge and experience and we cannot be held liable for any errors, inaccuracies, omissions or editorial failings that result from technological changes or research between the date of issue of this document and the date the product is acquired. Before using the product, the user should carry out any necessary tests in order to ensure that the product is suitable for the intended application. Moreover, all users should contact the seller or the manufacturer of the product for additional technical information concerning its use if they think that the information in their possession needs to be clarified in any way, whether for normal use or a specific application of our product. Our guarantee applies within the context of the statutory regulations and provisions in force, current professional standards and in accordance with the stipulations set out in our general sales conditions. The information detailed in the present technical data sheet is given by way of indication and is not exhaustive. The same applies to any information provided verbally by telephone to any prospective or existing customer.

# Text boxes

EVERBUILD 713 STANDARD SET FLEXIPLUS